## Slide 1
PhD Seminar
Biophysics, 4-1-12
Supervisor: K. Šipošová, PhD.
Consultant: A. Musatov, DrSc.
Evaluation of anti-amyloid and anti-oxidative activity of naked and surface-modified CeO2 nanoparticles

## Slide 2: Activities during the academic year 2020/2021
Research Activities:
i) Study of Bioactivity of CeO2-nanoparticles (CeO2-NPs)
evaulation of: a) pseudo-enzymatic activity - „catalase-" and "superoxide dismutase-like"
activity of CeO2-NPs;
b) effect of CeO2-NPs on insulin amyloid aggregation
ii) Preparation of surface-modified CeO2-NPs
iii) Examination of the detergent´s effect on amyloid aggregation
Others:
Completed of all exams (study part of PhD)
Preparation for dissertation exam and for defense of rigorous thesis
Participation at the conference
Participation in preparation of publications
PhD seminar, 16th June 2021

## Slide 3: Interplay between oxidative stress, aging and neurodegenerative diseases
Loss of protein homeostasis is a common feature of aging and diseases that are characterized by the appearance of nonnative protein aggregates in various tissues (Lévy, 2019)
One of the currently accepted theories is that oxidative stress is associated with aging processes and age-related neurodegenerative disorders, which are characterized by amyloid aggregation of proteins (Lévy, 2019; Butterfield, 1997)
several pathways linking
oxidative stress
neurodegenerative diseases
!!! the exact mechanism is unknown
PhD seminar, 16th June 2021

## Slide 4: CeO2 Nanoparticles for biomedical applications
shielded 4f-electrons and low redox potential of the Ce4+/Ce3+ redox couple (~1.52 V)
attractive optical, magnetic, and chemical properties
In collaboration with team of prof. Belous (Institute of Inorganic Chemistry NAS, Ukraine)
a new CeO2-NPs were prepared by controlled synthesis:
i) precipitation aqueous-alcoholic solutions: dd-H2O+Isopropanol (IPA) in precisely determined ratios
particles Ce1 – Ce5
ii) precipitation in a reverse microemulsion in the presence of Triton X-100 (CeO2)
CeO2 NPs | dTEM [nm] | w Ce3+ [%] | ζ-potential [mV] |  | 
 |  |  | H2O | 100 mM NaCl, pH 1.6 | + Insulin pH 1.6
Ce1 | 13,4±2,3 | 23 | +40,9 | +33,4 | +24,9
Ce2 | 8,0±0,8 | 30 | +41,5 | +35,3 | +28,9
Ce3 | 5,6±0,6 | 35 | +41,6 | +37,8 | +25,3
Ce4 | 3,5±0,4 | 38 | +42 | +36,9 | +29,5
Ce5 | 2,8±0,4 | 44 | +42,9 | +35,7 | +28,1
CeO2 | 5-6±1 | 28 | +46,9 | +36 | +26
X-ray diffraction (XRD) crystallographic analysis confirmed formation of fluorite Fm3m structure
XPS analysis allow to estimate the percentage of Ce3+ ions on the surface of CeO2-NPs
correlation between size and Ce3+/Ce4+ on the surface demonstrated
PhD seminar, 16th June 2021
SHLAPA Y.; TIMASHKOV I.; VELTRUSKÁ K.; ŠIPOŠOVÁ K.; GARČÁROVÁ I.; MUSATOV A.; SOLOPAN S.; KUBOVČÍKOVÁ M.; BELOUS A. Nanotechnology, 32, 31, 315706. 2021.

## Slide 5: Bioactivity of CeO2-NPs Pseudo-enzymatic activity
+
+
Oxidation
catalase-like activity
Catalase-like Activity
Catalytic activity of CeO2 NPs led to oxidation of N,N, Diethyl-p-phenylenediamine sulfate salt (DPD)
“true” catalase-like activity obtained by subtraction of kinetic curves without H2O2 from the kinetic curves with H2O2
PhD seminar, 16th June 2021
SHLAPA Y.; TIMASHKOV I.; VELTRUSKÁ K.; ŠIPOŠOVÁ K.; GARČÁROVÁ I.; MUSATOV A.; SOLOPAN S.; KUBOVČÍKOVÁ M.; BELOUS A. Nanotechnology, 32, 31, 315706. 2021.
Catalese like reaction
Oxidase like reaction

## Slide 6: Bioactivity of CeO2-NPs Pseudo-enzymatic activity
Superoxid Dismutase Activity
monitored using commercial SOD kit at two concentration of Ce1-Ce5: 50 and 75 µg/ml
SOD activity depends on size ⇒ the highest SOD-activity exhibited by the smallest, Ce5 nanoparticles (~ 2.8 nm)
SOD-activity is related to the content of Ce3+ ions – directly involved in reduction of O2- anion to H2O2
SOD activity of CeO2 NPs |  |  |  | 
 | 50 µg/mL |  | 75 µg/mL | 
 | % | U/mL | % | U/mL
Ce1 | 15.4±3.4 | 0.69±0.023 | 12.5±8.4 | 0.56±0.047
Ce2 | 18±4.9 | 0.81±0.04 | 13.7±8.1 | 0.61±0.05
Ce3 | 14.4±3.5 | 0.64±0.022 | 13.9±4.5 | 0.62±0.028
Ce4 | 18.4±4.3 | 0.83±0.03 | 25±3.6 | 1.18±0.05
Ce5 | 30.3±2.2 | 1.5±0.033 | 33±3.1 | 1.67±0.052
PhD seminar, 16th June 2021

## Slide 7: Bioactivity of CeO2-NPs Anti-amyloidogenic activity
CeO2-NPs
PDB 1GUJ (Ivanova, PNAS, 2009)
native proteins
effect on amyloid fibril formation
Inhibiting Activity
amyloid fibrils
effect on pre-formed amyloid fibrils
DisAssembly Activity
IC50 values
CeO2 NPs | 1200 rpm |  | 500 rpm | 
 | IC50 in µg/mL |  |  | 
 | ThT | ANS | ThT | ANS
Ce1 | 350±20 | 200±15 | 400±18 | 126±4
Ce2 | 310±10 | 200±10 | 390±15 | 140±8
Ce3 | 275±25 | 270±20 | 355±20 | 103±4
Ce4 | 165±15 | 95±6 | 183±9 | 70±4
Ce5 | 155±7 | 90±5 | 198±4 | 50±1.5
IC50 – CeO2 concentration caused a half maximal inhibition of protein amyloid aggregation
DC50 – CeO2 caused a half maximal disassembly of amyloid fibrils
QUANTIFICATION of Anti-Amyloid Activity
PhD seminar, 16th June 2021

## Slide 8: Bioactivity of CeO2-NPs Anti-amyloidogenic activity
The kinetics of insulin fibrillation in the presence of Ce1 particles (A) and in the presence of Ce5 (B) were monitored by fluorescent ThT analysis. The insulin concentration in the samples was always 25 µM.
PhD seminar, 16th June 2021
Time Dependence of Fibrils Formation
AFM Study of Anti-Amyloid Activity
Insulin fibrils (control)
1:0.8
1:0.02
1:2

## Slide 9: Preparation of surface-modified CeO2-NPs
Zeta-potential of naked CeO2 ζ = + 29.7 mV and ζ of surface-modified CeO2 ζ = + 22.1 mV
PhD seminar, 16th June 2021
CeO2 Synthesis*
Coating Using Detergent Dodecyl Maltoside, DDM
Characterization of CeO2 and CeO2-NPs@DDM
DDM adsorbed on CeO2-NPs: 10 mM DDM per 24 mg/mL CeO2-NPs
naked CeO2
24 hod./laboratory temperature
after incubation - particles separated by centrifugation and washed with MilliQ water (7x)
Wavenumber, cm-1
Absorbance
Bamd area/mA.cm-2
* SIPOSOVA K.; HUNTOSOVA V.; SHLAPA Y.; a kol. ACS Appl. Bio. Mater. 2019, 2, 5, 1884–1896.

## Slide 10: Bioactivity of surface-modified CeO2
Catalase-like activity - monitored using DPD assay
Left panel: Oxidation of DPD by CeO2-NPs in the presence (solid lines) and absence of H2O2 (dashed lines)
The “true” catalase-like activity of H2O2 decomposition by CeO2-NPs (right)
AFM Visualization of CeO2-DDM effect on insulin amyloid aggregation
CeO2-NPs@DDM at 1:2 ratios (protein:NPs).
IC50 [µg/mL] | CeO2 | CeO2-DDM
 | ~ 300 + 10 | ~ 260 + 17
PhD seminar, 16th June 2021
Anti-Amyloid Activity
Pseudo-Enzymatic Catalase Activity

## Slide 11
Summary:
PhD seminar, 16th June 2021

## Slide 12
Publications:
  SHLAPA, Yulia** - TIMASHKOV, Illia - VELTRUSKÁ, Kateřina - ŠIPOŠOVÁ, Katarína - GARČÁROVÁ, Ivana - MUSATOV, Andrey - SOLOPAN, Sergii - KUBOVČÍKOVÁ, Martina - BELOUS, Anatolii. Structural and physical-chemical characterization of redox active CeO2 nanoparticles synthesized by precipitation in water-alcohol solutions. In Nanotechnology, 2021, 32, 31, 315706.
Conferences:
Grants:
Grant Programme for SAS PhD Students, No. APP0164. "Study of anti-oxidant and enhanced anti-amyloid activities of cerium nanoparticles for biomedical applications"
G-5683 "Novel Composites Based on Cerium Oxide Nanoparticles and Carbon Enterosorbents for Acute Radiation Sickness Therapy"
VEGA-2/0009/17 "Functional and Structural Insights into the Phospholipid-Protein Interaction during Oxidative Stress"
APVV-19-0324 "The Development of Translationally Relevant Regenerative and Reparative Strategies After Spinal Cord Trauma"

## Slide 13
Anti-AMYLOIDOGENIC Activity
Anti-OXIDANT Activity
„pseudo“ catalase/peroxidase activity
„pseudo“ SOD activity
H2O2 + 2H+
H2O
2 O2- + 2 H+
O2 + H2O2
. . .
core/shell
Fe3O4@CeO2
Magnetic Delivery
AC magnetic Field HyperThermia
ferromagnetic
Future Plans:
PhD seminar, 16th June 2021

## Slide 14
Thank You for Your Attention